METALWORKING FLUID RECOMMENDATION CHART

| Product | Steel Alloys | Aluminum | Copper Alloys | Grinding | Milling, Turning | Boring, Drilling | Tapping, Threading | Sawing | Product Descriptions |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SYNTHETIC |  |  |  |  |  |  |  |  |  |
| Absolute Grinding Coolant | Yes | No | Yes | 4-6% | 5-7% |  |  |  | Grinding and metalworking fluid Low foam and mist Rust protection Economical Best choice for grinding shops |
| Hydro Cool MP | Yes | No | Yes | 4-6% | 4-6% | 6-8% | 7-9% | 6-8% | Machining fluid Low foam and mist Rust protection Excellent in central systems Good all around fluid |
| Super Synthetic Machining Fluid | Yes | No | Yes | 4-6% | 4-6% | 5-7% | 5-8% | 5-7% | Heavy duty synthetic Low foam and mist Rust protection For use where higher cutting power is needed |
| SEMI SYNTHETIC |  |  |  |  |  |  |  |  |  |
| Super Sawing Coolant | Yes | Yes | Yes | 4-6% | 4-6% | 6-8% | 7-9% | 6-8% | Machining fluid Rust protection Economical Good all around fluid |
| Ultimate SS | Yes | Yes | Yes | 4-6% | 4-6% | 5-7% | 5-8% | 5-7% | Machining fluid Low foam and mist Rust protection Excellent in central systems Better cutting power |
| Production SS | Yes | Yes | Yes | 4-6% | 4-6% | 5-7% | 5-8% | 5-7% | Machining fluid Rust protection Excellent in central systems High performance cutting Superior tool life |